# QUALITY ASSURANCE / QUALITY CONTROL PLAN (QCP)

# FOR Terrace Installation of EPDM membrane

QA/QC No.:									(1)  CLIENT : Shapoorji Pallonji

CONTRACT / W.O. NO.							              (2) INSPECTION AGENCY :

PROJECT :									(3) VENDOR / CONTRACTOR :

## Date :

| Sr.No | Component & Operation | Characteristics | Class | Type of check | Quantum of check | Reference documents | Acceptance Norm | Format of Record | Agency |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | P | W | V |
| 1. | Concrete Grade and surface finish to be applied | Physical | “CRITICAL” | Review | 100% | Test Report | Min. M 20 Grade PCC & with no surface defects ,sharp projection | STC | 3 | 1 & 2 | 1 & 2 |
| 2. | Material-EPDM membrane (a) Packing - Roll size (b) Grade | Physical … do .. | Major … do … | Visual …do … . | Random 100% | Mfg. Std …do… | Mfg. Std. … do… | Vendor STC | 3 | 2 | 1 |
| 3 | Application of EPDM membrane | Physical | Major | Visual | 100% | … do .. | … do .. | … do .. | 3 | 2 | 1 |
| 4 | a)Splicing of overlap joints with “BA” adhesive - 50mm min b) Use of “BA” for full bonding of EPDM membrane at all floor area | Physical ----do--- | Major ----do--- | Visual ----do--- | 100% ----do--- | … do .. ----do--- | … do .. ----do--- | … do .. ----do--- | 3 3 | 2 & 1 2 & 1 | 1 1 |
| 5 | ‘No Water / Rain’ Should fall during installation | Physical | “CRITICAL” - | Visual | 100% | Approved Application Procedure | Approved Application Procedure | Vendor STC | 3 | 2 | 1 |
| 6 | Job acceptance “Visual” | Physical | “CRITICAL” | Visual | 100% | Approved Application Procedure | No surface defects | Vendor STC | 3 | 2 & 1 | 2 & 1 |
| 7 | Final acceptance test: Water ponding for min 3 days. | Physical | “CRITICAL” | Visual | 100% | No water leakages | No water leakages | Vendor STC | 3 | 2 & 1 | 2 & 1 |

(P:   Performed by... W:  Witnessed by    V:  Verified by)   (1:  CLIENT….2:  INSPECTION AGENCY … 3:  VENDOR CONTRACTOR)

STC	:  Standard Test Certificate

Signature (Vendor)					        Signature (Inspection Agency)				Signature (CLIENT)

Note : 1)   Any special termination at pipe concrete interface to be pre approved by customer and record as acceptance criteria  .

2)    This formate should be based on approved method statement / application procedure